Supreme Garnet Technical Data Sheet:

# Text boxes

#### PHYSICAL CHARACTERISTICS :

Specific Weight		:	4.1 g/cm3

Average Bulk		:	2.4 g/cm3

Hardness		:	8 (Mohs Scale)

OTHER CHARACTERISTICS:

Crystal System	:	Cubic

Habit		:	Dodecadnedron with occasional

Trapezohedron

Fracture	:	Sub-Conchoidal

Durability	:	Very good

Free Flow	:	90% Minimum

Susceptibility to Acid	:	None

Moisture Absorption	:	Non Hygroscopic, Inert.

Magnetism	:	Very Slightly Magnetic

Conductivity	:	10 Microsiemens per Meter

Radio Activity	:	Not Detectable above background

Pathological Effects	:	None

Free Silica Content	:	None

Packing:

.25 Kg imported Multi-ply valve type paper bag

.25 Kg HDPE bag

.1 M.T and 2 M.T Jumbo bags

.40 x 25 Kg bags on shrink wrapped to pallets or to Jumbo bags

Special packing as per the customer requirement

#### MINERALOGICAL COMPOSITION

Garnet (Almandite)	:	97 – 98%

Ilmenite			:	1-2%

Quartz			:	½ %

Others			:	½ %

ANALYSIS & CHARACTERISTICS

ALUMINA	[ as Al2 O3 ]	:	21%

IRON     	[ as Fe2 O3 ]   	:	31%

SILICA	[ as Si O2 ]	:	35%

MAGNESIUM	[ as Mg O ]	:	8%

CALCIUM	[ as Ca O ]	:	1.5%

TITANIUM	[ as Ti O2 ]	:	1.0%

LEAD	[ as P2 O5 ]	:	0.05%

MANGANESE	[ as Mn O ]	:	0.5%

ZIRCON	[ as Zr O2 ]	:	Traces

CHLORIDE CONTENT	:	Less than 50 ppm

SOLUBLE SALTS		:	Less than 100 ppm

PH OF AQUEOUS MEDIUM	:	6.93

GYPSUM CONTENT	:	Nil

MOISTURE CONTENT	:	Less than 0.5%

CARBONATE CONTENT	:	Traces

LOSS ON IGNITION	:	Nil

METAL CONTENT		:	Traces [Specifically

Free Iron, Free Copper and

Other Heavy Metals]